## Slide 1: CARBON NANOSTRUCTURES (FULLERENES, CARBON NANOTUBES, GRAPHENE)
lecture for physics and chemistry students
(2020. summer semester – 17. February)
Prof. Jenő Kürti
ELTE Department of Biological Physics
e-mail: kurti@virag.elte.hu www: regivirag.elte.hu/kurti

## Slide 2
diamond sp3 graphite sp2
5.4 eV
1.7 eV
dCC  0,154 nm
dCC  0,142 nm
-16 meV / carbon atom
BAND STRUCTURE

## Slide 3
E
Egraphite < Ediamond

## Slide 4
E – TS
Egraphite < Ediamond Sgraphite > Sdiamond

## Slide 5
E – TS + pV
Egraphite < Ediamond Sgraphite > Sdiamond
Vgraphite > Vdiamond

## Slide 8
Downloaded from the internet

## Slide 9
DFT band structure of diamond

## Slide 10
DFT band structure of graphite

## Slide 11
Downloaded from the internet

## Slide 13
UNEXPECTED DISCOVERY in 1985
H.W.Kroto, J.R.Heath, S.C.O’Brien, R.F.Curl, R.E.Smalley,
„C60: Buckminsterfullerene”, Nature 318, 162 (14 Nov. 1985)
NOBEL-PRIZE: in 1996

## Slide 16
Richard E. Smalley (1943 – 2005)

## Slide 19
E.A.Rohlfing, D.M.Cox, A.Kaldor, J.Chem.Phys. 81, 3322 (1984)

## Slide 20
E.A.Rohlfing, D.M.Cox, A.Kaldor, J.Chem.Phys. 81, 3322 (1984)
H.W.Kroto, J.R.Heath, S.C.O’Brien, R.F.Curl, R.E.Smalley,
„C60: Buckminsterfullerene”, Nature 318, 162 (14 Nov. 1985)

## Slide 21
H.W.Kroto, J.R.Heath, S.C.O’Brien, R.F.Curl, R.E.Smalley,
„C60: Buckminsterfullerene”, Nature 318, 162 (14 Nov. 1985)
Curl
Heath
O’Brien
Smalley Kroto

## Slide 22
Truncated Icosahedron
Icosahedron

## Slide 24
R. Buckminster Fuller
American architect (1895-1983)
e.g. „geodesic dome” Montreal world exposition 1967

## Slide 26
Si-containing skeleton of the radiolarian Aulonia hexagona

## Slide 27
Notes: http://www.nanotech-now.com/Art_Gallery/chris-ewels.htm
Dreams of Buckminster Fuller "Buckminster Fuller, famous for his geodesic dome structures, once designed a dome large enough to cover mid-town Manhattan. Now his structures are reappearing in the chemistry of the nanoscale. So why not extrapolate a little?!"

## Slide 28
buckminsterfullerene
buckyball
(ballene
spherene
soccerene
carbosoccer ...)
C60
d  0,7 nm

## Slide 29
PRELUDE
PREHISTORY
…
ANTIQUE
– Babylon: „60”
– Greek:
Platon – 5 regular solids, including icosahedron
Archimedes – 13 archimedean solids, among which truncated icosahedron
Archimedes (287(?) - 212 B.C.)
Archimedes is believed to have conceived the thirteen "Archimedean solids", among which the truncated icosahedron is found.

## Slide 30
MIDDLE AGES
– 1480, Piero della Francesca – first known art of a truncated icosahedron
– 1498 or 1509, drawing from Leonardo da Vinci of a truncated icosahedron in Luca Paciolis book
– 1500, art from Albrecht Dürer of an outstreched truncated icosahedron
– XVI. c., truncated icosahedron in renaissance paintings
– China, Ming dynasty (1368-1644), lions sculpt, with his paw on a truncated icosahedron
– Topkapi Sarayi, part of a truncated icosahedron above a gate
– Japán „kagome” (triangle-hexagon) structures with pentagon (heptagon) substitution
(fairy-lamp)

## Slide 31
MIDDLE AGES
– 1480, Piero della Francesca – az első ismert rajz a csonkolt ikozaéderről
– 1498 vagy 1509, Leonardo da Vinci rajza csonkolt ikozaéderről Luca Pacioli könyvében
– 1500, Albrecht Dürer rajza egy kiterített csonkolt ikozaéderről
– XVI. sz., reneszánsz festményeken csonkolt ikozaéder
– Kína, Ming dinasztia (1368-1644), oroszlánszobor, mancsával csonkolt ikozaéderen
– Topkapi Sarayi, csonkolt ikozaéder részlet egy kapu fölött
– Japán „kagome” (háromszög-hatszög) szerkezetek ötszög (hétszög) helyettesítéssel
(lampion)

## Slide 32
Piero della Francesca (1420-1492)
This is oldest known picture of a truncated icosahedron (the shape of C60. It is from the book Libellus de quinque corpibus regularibus ("On the Five Regular Bodies"), by the Italian renaissance painter and mathematician Piero della Francesca.

## Slide 34
Leonardo da Vinci (1452-1519)
This rendition of the truncated icosahedron is from the book De Divina Proportione
("On Divine Proportion") by Fra' Luca Pacioli, published around 1498.
The drawing is ascribed to Leonardo da Vinci.
He seems to have invented this type of "skeleton model",
which lets us view both the outside and the inside of the polyhedron.
Johannes Kepler (1571-1630)
The concept of truncating a polyhedron was introduced by Johannes Kepler. Polyhedra were actually quite central to his research. In his work Prodromus Dissertationum Mathematicarum Continens Mysterium Cosmographicum ("The Cosmographic Mystery") he argued that the distances of the planets from the sun were determined by the Platonic solids.

## Slide 36
Fine Arts
An example of the appearance of the truncated icosahedron in art is shown in this picture from an Italian cathedral. At the top we see an icosahedron. It is bounded by twenty equilateral triangles. At each of the 12 vertices of the icosahedron, five of the triangles meet. Cutting off ('truncating') these vertices thus replaces each of them by a pentagonal face; it also converts each of the twenty former triangular faces into a hexagon. We can see the resulting truncated icosahedron at the bottom of the picture. This is the shape of the C60 molecule.

## Slide 40
XX. century
– 1933, László Tisza icosahedral point group
– 1942, D.W. Thompson: carbon cage of 12 pentagons + any number of hexagons
– 1965, Schultz, from geometrical considerations: C60H60 – truncated icosahedron
– 1966, David Jones („Daedalus”), in New Scientist: football shaped carbon molecule from hexagons (intermediate density)
– Buckminster Fuller (1895-1983), geodesic buildings
– 1970, Eiji Osawa, Kagaku-ban (Yoshida): possibility of 3D aromatic structures  C60
(– 1971, W.E. Barth és R.O. Lawton, synthesis of corannulene)
– 1973, D.A. Boc’var and G.E. Gal’pern, generalizatoin of ferrocene structure  C20 (suggestion of Stankevic’: C60)
– 1980, S. Iijima, with electron microscope: spherical carbon particles from carbon evaporated in vacuum
– 1981, R.A. Davidson, Hückel calculations on carbon clusters, also on C60
– 1983, L.A. Paquette, C20H20 synthesis (dodecahedron)
– 1981-85, O. Chapman, tried to synthesize C60 – without success
– 1985 september Kroto, Smalley, Curl, …
– 1985 október 9., A.D.J. Haymet, Hückel calculations on C60

## Slide 42
corannulene