## Slide 1: CARBON NANOSTRUCTURES (FULLERENES, CARBON NANOTUBES, GRAPHENE)
lecture for physics and chemistry students
(2020. summer semester – 04. May)
Prof. Jenő Kürti
ELTE Department of Biological Physics
e-mail: kurti@virag.elte.hu www: regivirag.elte.hu/kurti

## Slide 2
C60 superconductivity

## Slide 4
RbCs2: 33K
1st:
2nd:

## Slide 5
RbCs2: 33K

## Slide 6
C60 polymers

## Slide 7
Woodward-Hoffmann rules
(4n, 4n+2 …)
Photopolymerization
Ionic polymerization
High pressure polymerization
[2+2] cycloaddition

## Slide 8
Kováts Éva PhD értekezés, 2006
Symmetry of the molecular orbitals in the transient state during dimer formation.
Upper part: LUMO, lower part: HOMO

## Slide 9
Oszlányi Gábor MTA doktori, 2005
[2+2] cycloaddition
C60 – C60 distance (Å)
high pressure mechanism
neutral
ionic mechanism
or
photoreaction

## Slide 10
Photopolymerization

## Slide 14
Several possible C60 – trimers
[2+2] cycloaddition C60 – dimer (D_D2h)

## Slide 15
Number of vibrations for two independent C60:
2 x (3 x 60 – 6) = 348
Number of vibrations for C60 dimer:
(3 x 120 – 6) = 354
→ there are 6 extra vibrations
CAN YOU EXPLAIN WHY?
CAN YOU IDENTIFY THE SYMMETRY OF THEM?

## Slide 16
Ionic polymerization

## Slide 18
C60 ionic polymers
: A: alkali atom (Na, K, Rb, Cs)
A1C60
[2+2] cycloaddition
D2h
9.14 Å

## Slide 26
Pekker et al.

## Slide 27
Pekker et al.

## Slide 29
High pressure polymerization

## Slide 30
1D – 2D

## Slide 31
Kováts Éva PhD értekezés, 2006

## Slide 32
C60 – cubane

## Slide 33
Kováts Éva PhD értekezés, 2006
Cubane (C8H8)
sigma-skeleton space filling model

## Slide 34
Kováts Éva PhD értekezés, 2006
C60–cubane microcrystals in reflection microscope. 1 division: 2μm.

## Slide 35
Kováts Éva PhD értekezés, 2006
„rotor – stator” system
Structure of C60 – cubane molecular crystal

## Slide 37
Endohedral fullerenes

## Slide 38
Endohedral fullerenes, e.g. N @ C60

## Slide 39
N @ C60
Sc @ C82

## Slide 40
Sc @ C82
Er3N @ C80

## Slide 41
At the end two comments:
Fullerenes were discovered by chance, the motivation came from astrophysical – astrochemical ideas. It is interesting to mention, that more than two decades after the discovery of fullerenes it turned out that C60 and C70 can be indeed observed in the interstellar space. See e.g. Jan Cami et al., „Detection of C60 and C70 in a Young Planetary Nebula”, Science 329, pp 1180-1182 (2010).
An amazing experiment was done in 1999 at the University of Vienna: interference pattern was observed in a double slit arrangement with C60 molecules. Fullerene molecules are one of the largest objects for wich the particle – wave duality has been demonstrated. See e.g. M Arndt et al., „Wave-particle duality seen in carbon-60 molecules”, Nature 401, p680 (1999).